Two-Photon Source in the Telecom Band

Tae-Gon Noh, Heonoh Kim, Chun Ju Youn, and Seok-Beom Cho

IT Convergence Technology Research Division, Electronics and Telecommunications Research Institute, Daejeon 305-350, Korea

The generation of correlated photon pairs in the telecom band is of particular interest for future applications with low-loss standard optical fibers. Here we show a source of noncollinear correlated photon pairs in the 1550 nm band using a spontaneous parametric down-conversion process. Within the band, the source gives a completely flexible choice of the frequencies of the photon pairs, and correlation properties related to spatial momentum as well as energy and time can easily be utilized. We characterize the source by measuring the spatial intensity distribution of the down-converted light and by performing coincidence counting.